## Slide 1
Current status of QCS upgrade
Michinaka SUGANO
Cryogenics Science Center, KEK
On behalf of the QCS group
October 26, 2026
ARC

## Slide 2
Acknowledgement
• KEK (in particular)
N. Ohuchi, Y. Arimoto, K. Aoki, K. Suzuki, H. Yamaoka, X. Wang, T. Oki, T. Nakamoto, T. Ogitsu, R. Bajpai
• Sophia University: Characterization of Nb3Sn wires, simulation of magnetic field decay
S. Hoshino, K. Kaneko, T. Yagai
• Furukawa Electric: R&D of Nb3Sn wires
K. Mun, R. Taniguchi
• FNAL: Technical support for the Nb3Sn QC1P development
S. Stoynev, V. Kashikhin, G. Ambrosio, M. You, S. Krave, X. Xu, G. Velev, S. Gourlay
• BNL: Design for corrector magnets
V. Teotia, B. Parker

## Slide 3
Contents
• Answers to recommendations from the reviewers at the last ARC
• Overview of the QCS upgrade
• Nb3Sn QC1P development
• Corrector magnets and compensation solenoid

## Slide 4
Answers to recommendations from the reviewers at the last ARC
R15.2: Complete the study of whether the radiation doses to the SC magnet coils due to SBLs, other beam aborts, and accumulated backgrounds will ultimately degrade the integrity of the SC magnet.
R22.2: Before embarking on the manufacture of tooling, study the possibility and implications of using a two-layer coil, and compare manufacturing, cost and performance issues with those associated with the single layer coil design shown in the presentation.
After the last ARC, we discussed which coil design option to choose within our group and FNAL. Then, we concluded that, in such a small coil, there will be a risk of mispositioning of the Nb3Sn wire and insulation damage in a two-layer coil. Thus, we prioritized R&D for single-layer coils. We are repeating the fabrication of practice single-layer coils, but we have recognized some difficulties such as mispositioning of the ramp lead. In parallel with developing the single-layer coils, we have started R&D for two-layer coils. We will report on the results of the first practice winding for a two-layer coil in this presentation.
We have answered this comment in the previous talk given by Arimoto.

## Slide 5
Overview of the QCS upgrade

## Slide 6
Why is the QCS upgrade needed?
– Main quadrupoles are exposed to the detector solenoid field in the current QCS
QC1RP
QC1LP
Belle solenoid field
IP
LER
HER
QC2RP
Correctors
QC1RE
Correctors
QC2RE
Correctors
QC2LP
Correctors
QC1LE
Correctors
QC2LE
Correctors
Compensation solenoid
Install the main quadrupoles with rotation and offset
Large chromatic x-y coupling
Layout of current QCS
 IR optics need to be simplified.
– Moving QC1P forward to IP
Larger dynamic aperture and longer beam lifetime were expected in an early study.
A more severe space constraint  Replacing Nb-Ti coils with Nb3Sn coils having a higher critical current density
– Mitigation of beam-induced quench
Larger temperature margin by adopting Nb3Sn with a higher critical temperature
Correctors
Correctors

## Slide 7
QCS upgrade
100 mm
Extension of
compensation
solenoid
Move QC1P forward
closer to IP
QC1LP
QC2LP
QC2LE
QC1LE
QC1RP
QC1RP
QC1RE
QC2RE
Corrector
magnet
Corrector
magnet
Current
QCS
Upgraded
QCS
Compensation solenoid
• Extension of compensation solenoid
LER
HER
IP
IP
The detector solenoid field is canceled ahead of QC1P.
 Simplified IR optics
• Place Nb3Sn QC1P with iron yoke 100 mm closer to IP
 Thinner coil size, larger temperature margin
Lower operating current, reducing magnetic crosstalk to HER
by iron yoke

## Slide 8
Current QCS
QC2LP
Correctors
QC2LE
Correctors
QC1LE
Correctors
Correctors
QCS-L Cryostat
QCS-R Cryostat
HER
LER
QC1LP
QC1RP
QC1LE
Correctors
QC2RP
Correctors
ESL solenoid
ESR1 solenoid
ESR2
ESR3
Extended
compensation solenoid
He Vessel
He Vessel
He Vessel
QC2RE
Correctors
IP
Layout of QCS magnets
He Vessel
Main changes in upgraded QCS
• Extension of compensation solenoid
• Relocation of QC1P with iron yoke
(Nb3Sn is the baseline, Nb-Ti as a backup)
• New correctors for QC1P
• No leak field cancel coils
*Multipole order of correctors
has not been fixed.
Correctors
Main quadrupoles |  |  | 
 | Field gradient (R, L) (T/m) | Design current, Id (R, L) (A) | Peak field at Id (R, L) (T)
QC1P | 76.37 | 1800 | 4.56
QC1E | 91.57 | 2000 | 3.50
QC2P | 31.97 | 1000 | 2.43
QC2E | 38.56, 36.39 | 1562.5, 1250 | 2.81, 2.63
Compensation solenoids |  |  | 
 | Design current, Id (A) | Peak field at Id (T) | Coil inner radius (mm)
ESL | 390 | 3.56 | 78~(145)
ESR1 | 450 | 3.05 | 70~189
ESR2 ESR3 | 151.1 | 0.3 T | 81.1
Specifications of magnets for the current QCS
Upgraded QCS
(tentative)

## Slide 9
Tentative schedule of QCS production
 | FY2026 | FY2027 | FY2028 | FY2029 | FY2030 | FY2031 | FY2032 | FY2033 | FY2034 | FY2035
QC1P |  |  |  |  |  |  |  |  |  | 
Corrector magnet |  |  |  |  |  |  |  |  |  | 
Compensation solenoid |  |  |  |  |  |  |  |  |  | 
Cryostat |  |  |  |  |  |  |  |  |  | 
QCS system including main quadrupoles other than QC1P |  |  |  |  |  |  |  |  |  | 
Run2
Run3
LS2
R&D magnet 2
in case of Nb3Sn
R&D magnet
in case of Nb-Ti
Test and review
of QC1P proto
Development
of Nb3Sn QC1P
(Nb-Ti as a backup)
Production of
QC1LP, RP
Production of QCSL
Production of QCSR
Belle
roll-in
Design of QCSL/R cryostat
Specifications
Design and
production of R&D
magnets
with a company
Specifications for
production of QCSL, R
Bid for production
of QCSL, QCSR
Design of
corrector magnets
Production of corrector magnets
for QCSL, R
Bid for corrector magnets
for QCSL, R
Design of corrector magnets
R&D of Nb3Sn
solenoid, test
Bid for
QC1LP, RP
Production of
QC1P proto
by KEK
Bid for compensation
solenoids
Production of QCSL, R
compensation solenoids
QCSL test
on the ground
QCSL
installation to beam line,
test, alignment
MFM
Production of supplies
Production of supplies
QCSR
installation to beam line,
test, alignment

## Slide 10
Nb3Sn QC1P development

## Slide 11
New Nb3Sn QC1P
 | Units | Present | Upgrade
Conductor material |  | Nb-Ti | Nb3Sn
Integral Gradient | T | 22.96 | 26.7
Operation current | A | 1600 | 1832
Field gradient | T/m | 68.74 | 80
Field Quality |  | < 10-4 | 
Material of magnetic yoke |  | - | Iron
Inner radius of coil (1st layer) | mm | 25.0 | 22.5
Outer radius of coil (1st layer) | mm | 27.65 | 24.2
Inner radius of coil (2nd layer) | mm | 27.78 | -
Outer radius of coil (2nd layer) | mm | 30.43 | -
Inner radius of collar or yoke | mm | 30.75 | 26.25
Outer radius of collar or yoke | mm | 35.5 | 40.0
Physical length | mm | 409.3 | < 400
Effective magnetic length | mm | 333.6 | 334
Stored energy | kJ | 1.43 | 0.484
Inductance | mH | 0.88 | 0.29
Cross sectional size of strand | mm | Φ 0.498 | 0.8 x1.5
Cu/SC ratio |  | 1 | 0.83
Filament diameter | µm | 7.7 | < 5
Number of strands |  | 10 | 1
Cable width | mm | 2.5 | 1.5
Cable thickness | mm | 0.93 | 0.8
Magnet operation temperature | K | 4.7 | 4.7
Load line ratio | % | 72 | 80
Temperature margin to Tcs | K | 1.9 | 4.6
Ic at 7 T, 4.2 K | A | 193 | -
Ic at 12T 4.2 K | A | - | > 500
Main Design Parameters of QC1P (Tentative)
R25
R22.5
Current QC1P
Nb3Sn QC1P (tentative)
• The coil thickness needs to be reduced to install the magnet into
a narrower space
– Nb3Sn monolith wires will be used instead of Nb-Ti Rutherford
cables
– Two options for the coil design: single-layer or two-layer
• Collaring with iron yoke
– Coil pre-stress as high as 100 MPa during assembly to keep the
Nb3Sn coils in compression after cooling
Stainless steel collar
2.5 mm
0.93 mm
1.5 mm
0.8 mm
Iron yoke
Nb-Ti
Rutherford
cable
Nb3Sn
monolith
wire

## Slide 12
Coil design: Single-layer or Two-layer
Single-layer coil
Pros
• Simple coil winding
• A thinner coil
Cons
• Higher operating current and smaller temperature
margin than that of two-layer coils
• Position control of ramp lead
• Difficult mechanical support for ramp lead
Two-layer coil
Pros
• Lower operating current and larger temperature margin
• Easy lead support
• Layer jump can be placed at the coil end.
Cons
• More complex coil winding, which can cause misalignment of turns
• A risk of wire insulation damage during coil winding
Both options have pros and cons.
We will decide which coil design to choose after the mirror magnet tests.
Single-layer
Two-layer
Ramp lead of a single-layer coil

## Slide 13
Flow of the Nb3Sn QC1P development
Establishment of coil fabrication technology
Individual performance test of coils using a mirror magnet
Selection of either single-layer coil or two-layer coil
Review of Nb3Sn QC1P at the end of FY2027
(If the technical maturity of the Nb3Sn magnet is deemed insufficient,
we will switch to the Nb-Ti option.)
Fabrication of R&D quadrupole magnet, Performance verification test

## Slide 14
Wire with a keystone angle
Rectangular wire for R&D
200 mm
Reduction in the time decay of the magnetic field  Fine filaments
Large pre-stress during assembly  CuNb-reinforced wire
Size： 0.80±0.02 mm x 1.50±0.02 mm
Areal ratio： non-Cu 50±5%, CuNb 23±5%, Cu 27±5%
Filament diameter： 2.3 mm（nominal）
Reinforcer： CuNb（Cu-20vol%Nb）
Barrier： Ta
Insulation：S-2 glass braid
Size of insulated wire：1.00±0.035 mm x 1.70±0.035 mm
Ic at 12 T, 4.2 K: >500 A
RRR： >100
• Furukawa Electric fabricated Nb3Sn wire with a keystone angle
of 2.29o as a trial.
• Quench occurred during Ic measurements for short straight samples.
A further study will be conducted at KEK.
Cu
CuNb
Ta
Nb + Bronze
CuNb-reinforced Nb3Sn wire

## Slide 15
Structure of single-layer coil
• Coil inner radius: 22.375 mm, coil outer radius: 24.525 mm
• Coil mechanical length: 441 mm
• Number of turns: 11
• Insulation
– Double S2-glass sleeves for the pole and mid-plane turn
– S2-glass sheet for thickness compensation
– S2-glass sheet to cover the inner and outer surfaces
• A G10 cover is impregnated with a coil for mechanical support
of the ramp lead.
S2-glass sleeve: t0.1 mm
Double S2-glass sleeves: t0.1 mm x 2
S2-glass sheet: t0.125 mm
S2-glass sheet
for thickness compensation:
t0.125 mm
S2-glass sheet: t0.125 mm
Ti-alloy pole
Nb3Sn wire
Splice
441 mm
G10 cover

## Slide 16
Fabrication of single layer Nb3Sn coils
Coil winding
Heat treatment
Epoxy impregnation
• A coil is not cured before reaction.
• Multi-step heat treatment over 2 weeks
(Max. temperature = 650oC)
• Impregnation with CTD-101K (Epoxy
resin)

## Slide 17
Practice coils
(Single-layer
coils)
PC1
PC2
PC3
ID | Purpose | Insulation between pole turn and Ti-alloy pole | Heat treatment | Epoxy | Electrical test result (Hi-pot test btw pole and conductor)
PC1 | Check winding, heat treatment, and epoxy impregnation tooling | Single S2 glass sleeve | Shortened pattern | EPO-TEK 301 | Electrically shorted in a Hi-pot test  NG
PC2 | Slightly modified tooling to accommodate additional glass sleeve, check the electrical insulation | Double S2 glass sleeves | Shortened pattern | EPO-TEK 301 | Leak current of 15.7 mA at 1  NG
PC3 | The same tooling as PC2, check the electrical insulation, first coil impregnated with CTD101-K | Double S2 glass sleeves | Shortened pattern | CTD101-K | No leak current at 2 kV  OK
PC4 | Minor modification from the tooling for PC3, full reaction for coil size measurement, electrical test | Double S2 glass sleeves | Full reaction | CTD101-K | Leak current of 206 mA at 0.09 kV  NG
PC4
The coil fabrication
process has not been
fully established.
Ti-alloy pole
Nb3Sn wire
Cross-section
of PC3

## Slide 18
Groove for layer jump
R&D of two-layer coil
• Practice winding of a two-layer coil with 3D-printed parts has started.
• Each layer was temporarily secured by instant glue to simulate the curing process.
• The layer jump lead could be wound along the groove located at the coil end.
• Design of coil fabrication tooling for two-layer coils will start soon.
Location of the layer jump

## Slide 19
Mechanical structure of mirror magnet
Top block
Bottom block
Pushing
block
Temporary shim
during coil insertion
(SUS304)
Final shim
(Iron)
Fixing part (SUS304)
Nb3Sn coil
Mid-plane block (Iron)
Load-bearing bolt
(SUS316L)
Coil fixing bolt (SUS304)
• A “Mirror magnet” can reproduce the magnetic field distribution and Lorentz force within a quadrupole magnet.
 Relatively easy performance test for a Nb3Sn coil
• Monitoring coil stress during assembly, cooldown, and excitation by strain gauges
 Verify the validity of the mechanical design for brittle Nb3Sn coils
• Training performance will be checked by excitation tests at 4.2 K.
2D cross-section
3D model with end structure

## Slide 20
Magnetic design of mirror magnet
A mirror magnet reproduces a similar magnetic field distribution
and the stress of a quadrupole magnet.
ANSYS simulation for more detailed structural analysis is ongoing.
Y. Arimoto
Operating current
Operating current
Bmax (G)
Current (A)
Current (A)
Lq (N/cm)
Operating current
Pole turn
MP turn
Quadrupole
magnet
Mirror
magnet
Pole turn
MP turn
Quadrupole
magnet
Mirror
magnet
2.5 T
0 T
Quadrupole magnet
Mirror magnet
• Difference in magnetic field within a coil between a quadrupole magnet
and a mirror magnet < 0.25%
• Difference in Lorentz force exerted on a coil between a quadrupole magnet and a mirror magnet ~3%

## Slide 21
Corrector magnets and compensation solenoid

## Slide 22
Corrector magnets
Required corrector magnets
• Corrector coils for main quadrupoles other than QC1P
– Almost the same design as those for the current QCS
• Corrector magnet for new QC1P
– Limited longitudinal space  Higher magnetic field to keep the same field integral
• Required multipole orders of the correctors and field integral for each coil are being discussed with the optics team.
Strategy for design and fabrication
• Correctors for the current QCS were designed and fabricated by BNL based on the direct winding technology.
• In the QCS upgrade, BNL is responsible only for the design of the correctors, while a Japanese company will
manufacture the magnets.
• KEK plans to place an order for a trial fabrication of corrector coils with the candidate company in FY2027.
Corrector coils (a1, b1, a2, b4)
Direct winding technology developed by BNL
Design study for corrector magnet for new QC1P
Cross-section of current QC1E
Main
quadrupole
coils

## Slide 23
Compensation solenoid
• The front end of the extended compensation solenoid will be made of Nb3Sn
for a smaller coil size and mitigation of beam-induced quench.
• Nb3Sn “solenoid coils” are widely used in commercial products.
• Assuming the same Nb3Sn wire as QC1P
• A design study has started for ESL for QCS-L.
• Thinner coil with a comparable current margin and
a larger temperature margin in the Nb3Sn option than in the Nb-Ti one
• For the rest of the compensation solenoid, Nb-Ti coils will be adopted,
which is the same as the current QCS.
NbTi: current margin 35%
Nb3Sn: current margin 40%
Magnetic design of the extended ESL
Front end of the extended
compensation solenoid
Front end of the extended
compensation solenoid
Bpeak=3.21 T at J=304 A/mm2
Bpeak=3.39 T at J=631 A/mm2
23.6 mm
16.6 mm
Nb3Sn coil
Nb-Ti coil
LHe vessel
Tmargin=2.1 K
Tmargin=7.6 K
Nb3Sn
Nb-Ti
Critical current – magnetic field curves
4.7 K
4.7 K
12.3 K
6.9 K
Tmargin

## Slide 24
Summary
• QCS upgrade is planned during LS2. The main changes include the extension of the compensation
solenoid, moving QC1P with Nb3Sn coils forward to the IP, and a new corrector magnet for QC1P.
• R&D on Nb3Sn QC1P is currently underway at KEK. If the technical maturity of the Nb3Sn magnet is
deemed insufficient at the end of FY2027, we will switch to the Nb-Ti option.
• BNL is responsible for the design of corrector magnets, while a Japanese company will manufacture the
magnets.
• The Nb3Sn option will be adopted for the front end of the extended compensation solenoid, considering
a thinner coil size and larger temperature margin.

## Slide 26
Appendix

## Slide 27
Plan for electrical test
• Coil resistance
before splice
after splice
• Coil inductance
• Hi-pot test
Voltage is applied between Ti-pole and wire.
Max voltage estimated from quench simulation: 184 V (Kento Suzuki, “QC1P_250521.pptx”)
Criteria adopted for HL-LHC magnets
– Max voltage: (184 x 2 + 500) x 2 =1736 V  1.8 kV
– Leak current < 10 mA
– Duration time = 30 sec
• Impulse test
184 / 4 = 46 V/coil
Max voltage: (46 x 2 +500 ) x 2 = 1184 V  1.2 kV
We need to check if the max current during the test is acceptable.

## Slide 28
Magnetic design of single-layer coil (2D, 3D)
Single-layer coil
G10 cover
• Epoxy impregnation with a G10 cover
• Enlargement of yoke inner diameter
to 26.25 mm
R26.25 mm
R40 mm
25.4606°
2.2694°
2.5461°
R23.35 mm
13.75 mm
SingleLayer_v1
SingleLayer_v2
R24.7 mm
R40 mm
25.4606°
2.2694°
2.5461°
R23.35 mm
15.3 mm
 | SingleLayer_v1 |  | SingleLayer_v2 | 
 | 2D | 3D | 2D | 3D
Yoke ID (mm) | 24.7 |  | 26.25 | 
Yoke OD (mm) | 40 |  | 40 | 
Bmax (T) | 2.47 | 2.84 | 2.47 | 2.77
I at G=80 T/m (A) | 1656 | 1658* | 1831 | 1832*
J (non-Cu) (A/mm2) | 2760 | 2763 | 3052 | 3054
Load line ratio | 0.72 | 0.76 | 0.76 | 0.80
Rin=26.25 mm
Rin=24.7 mm
2D
* Current at G=80 T/m at the longitudinal center
of the straight section

## Slide 29
Two layer magnet is designed with 2D analysis.
Number of turns
  – 11 turn (inner coil)
  – 12 turn (outer coil)
Inner radius
  – 22.6 mm (inner coil) (same as single-layer magnet)
  – 24.4 mm (outer coil)
22.6 mm
24.4 mm
R26.8 mm
R41.8 mm
Two-layer magnet
 | I (A) | A (mm2) | J nc (A/mm2) | B2 (T) | b6 (units) | b10 (units)
Single-layer | 1700 | 1.2 | 2833 | 0.8042 | 0 | -2.2
Two layer (12 turn) | 920 | 1.2 | 1533 | 0.8017 | -0.1 | -1.7
Two layer (11 turn) | 960 | 1.2 | 1600 | 0.8040 | 0 | -1.9
Rref = 10 mm
Jnc is half the value of the single-layer option.
Bpeak = 2.3 T

## Slide 30
4.7 K
6 K
7 K
8 K
9 K
10 K
11 K
12 K
13 K
9 K
8 K
7 K
6 K
4.7 K
One layer magnet
Two layer magnet
Current QC1P
Operation points
 | Temperature margin (K) | 
 | Nb3Sn | NbTi
Single-layer | 4 | 1
Two-layer | 8 | 2.5
Current QC1P | - | 2
Critical surface and operation points
• The operating point of the two-layer magnet
moves to the lower J region.
• The temperature margin increases by twice
for Nb3Sn.

## Slide 31
Location of electrical short in PC4
V1
Ti pole
Nb3Sn conductor
Ramp lead
MP lead
Splice
Splice
Nb-Ti Rutherford cable
I
I
X
Electrical
short
Ramp lead side
V2
1
2
If an electrical short is located between Points 1 and 2,
a sign of V1 and V2 is reversed.
1
2
3
4
5
6
7
8
• The location of an electrical short was identified between 5 and 6 by a voltage measurement.
Resin and glass insulation were removed at Points 1-8 to measure the voltage
between the pole piece and the conductor.
Zero-crossing
Approximate location of electrical short

## Slide 32
Corrector magnets in the current QCS
 | Multipole orders
QC1P | a1, b1, a2, b4
QC1RP | a1, b1, a2, b4, b3*
QC1LE | a1, b1, a2, b4
QC1RE | a1, b1, a2, a3
QC2LP | a1, b1, a2, b4
QC2RP | a1, b1, a2, a3
QC2LE | a1, b1, a2, b4
QC2RE | a1, b1, a2, a3
QC1-2RE | b3
QC1-2RP | b3

## Slide 33
Possible reason for mispositioning of ramp lead
Before epoxy impregnation, a coil is completely released from the heat treatment jig, and then the coil is turned
upside down to put a glass sheet on the coil inner surface. Since the coil is not cured, the ramp lead would be
easily twisted.  Curing would be necessary even for a single-layer coil.